Standard PVDF Colors (24 & 22 Gauge) Dura Tech® 5000

Cool Regal White *
SRI: 88 • LRV: 75

Cool Parchment
SRI: 58 • LRV: 40

Cool Sierra Tan
SRI: 55 • LRV: 34

Cool Walnut
SRI: 38 • LRV: 18

Cool Weathered Copper
SRI: 34 • LRV: 11

				

Cool Dark Bronze
SRI: 32 • LRV: 8

Cool Terra-Cotta
SRI: 41 • LRV: 15

Cool Colonial Red
SRI: 35 • LRV: 9

Cool Old Town Gray
SRI: 43 • LRV: 27

Cool Zinc Gray
SRI: 39 • LRV: 20

				

Cool Slate Gray
SRI: 33 • LRV: 12

Cool Midnight Bronze
SRI: 27 • LRV: 7

Cool Matte Black *
SRI: 29 • LRV: 5

Cool Tahoe Blue
SRI: 33 • LRV: 14

Cool Regal Blue
SRI: 29 • LRV: 10

Cool Leaf Green
SRI: 30 • LRV: 11

Cool Forest Green
SRI: 29 • LRV: 9

Engineered to Perform. Designed to Inspire.
This modern curated color palette delivers durable, vibrant finishes with long-lasting performance. Each refined color is listed with the Cool Roof Rating Council (CRRC) for energy efficiency and supports sustainability targets so you can design and build with confidence.

Metallic PVDF Colors (24 & 22 Gauge) Dura Tech® mx Subject to upcharge.

Cool Metallic Silver 1
SRI: 65 • LRV: 50

Cool ZACtique® II 1
SRI: 39 • LRV: 22

Cool Metallic Champagne 1
SRI: 54 • LRV: 33

Cool Metallic Copper 1
SRI: 53 • LRV: 29

Contact AEP Span

Premium Colors (Gauge Varies) Subject to upcharge.	Unpainted Products (Gauge Varies)

Vintage® 1
SRI: 22 • LRV: 20

Carbon - Natural Matte®
SRI: NA • LRV: 4

Shale - Natural Matte®
SRI: 41 • LRV: 23

ZINCALUME® Plus 1
SRI: 64 • LRV: 67

Pre-Primer
Pre-Primed Both Sides

Custom Colors Available By Special Order

Inquire with your sales representative for lead times and minimum order requirements.

www.aepspan.com

Premium Metal Roofing & Siding

Architectural Color Chart

®

Vintage® : 24ga finish with a FEVE paint system and TruZinc® G90 substrate.
ZINCALUME® Plus : 24-20ga bare, unpainted with a clear acrylic coating.
* Available in .040” Aluminum : Stocked dual-sided with Matte Black on one side and Regal White on the other.

Natural Matte® : 24-22ga ultra low-gloss finish with a PVDF paint system and ZINCALUME® substrate.
Pre-Primer : 24ga pre-primed both sides for field painting.
1 Batch Sensitivity : Finishes are batch sensitive (may have color variation) and directional. Different batches should not be mixed on projects.

Premium Metal Roofing & Siding
Color & Product Matrix	®

TABLE NOTES:
24ga & 22ga
24ga Only
22ga Only
24ga, 22ga, & 20ga

Standard PVDF Colors — Dura Tech® 5000

PAINT SYSTEM OVERALL PRICE POINT WARRANTY DURABILITY

SRI: Solar Reflective Index LRV: Light Reflectance Value Design Span® hp
Span-Lok™ hp & SpanSeam™ Select Seam®
Flex Series Prestige Series®
Perception Collection® Flush Panel
HR-36®
Box Rib™
Nu-Wave® Corrugated PBR Panel
U-Panel
Flat Sheet 46” Flat Sheet 48 3⁄8”

APPLICATION

SMP
Better Moderate Long
Good Weatherability
Residential & Light-

PVDF
Best Higher Longest
Superior Weatherability
High-end, Architectural,

Cool Regal White *
Cool Parchment
Cool Sierra Tan

88  75  ●  ●  ●

58 40  ●  ●  ●
55  34  ●  ●  ●

●	●  ●  ●
●	●  ●  ●
●	●  ●  ●

●  ●  ●  ●  ●
●  ●  ●  ●  ●
●  ●  ●  ●  ●

OTHER ATTRIBUTES

Commercial
Wide Range of Color & Gloss Options

& Commercial
Excellent Chalk & Fade Resistance

Cool Walnut
Cool Weathered Copper
Cool Dark Bronze Cool Terra-Cotta Cool Colonial Red Cool Old Town Gray Cool Zinc Gray
Cool Slate Gray
Cool Midnight Bronze Cool Matte Black * Cool Tahoe Blue
Cool Regal Blue
Cool Leaf Green
Cool Forest Green

38  18  ●  ●  ●
34  11  ●  ●  ●
32  8  ●  ●  ●
41  15  ●  ●  ●
35  9  ●  ●  ●
43  27  ●  ●  ●
39  20  ●  ●  ●
33  12  ●  ●  ●
27	7	●  ●  ●
29  5	●  ●  ●
33  14  ●  ●  ●
29  10  ●  ●  ●
30  11  ●  ●  ●
29  9  ●  ●  ●

●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●
●	●  ●  ●

●
●  ●  ●
●  ●  ●
●  ●  ●
●  ●  ●
●  ●  ●
●  ●  ●
●  ●  ●
●
●  ●  ●
●  ●  ●
●  ●  ●
●  ●  ●
●  ●  ●

● Dura Tech® 5000 : A premium 70%
●  Polyvinylidene Fluoride (PVDF) paint system.
Dura Tech® mx : A premium 70%
● Polyvinylidene Fluoride (PVDF) Pearlescent
● paint system.
● Vintage® : 24ga finish with a FEVE paint system on a TruZinc® G90 substrate with
● graffiti-resistant qualities.

●  ●

● Natural Matte® : 24 & 22ga ultra low-gloss finish with a PVDF paint system on a ZINCALUME® substrate.
● ZINCALUME® Plus : 24-20ga bare, unpainted
● with a clear acrylic coating.
● Pre-Primer : 24ga pre-primed both sides for field painting.
● * Available in .040” Aluminum : Stocked
●  dual-sided with Matte Black on one side
●  and Regal White on the other.

Metallic PVDF Colors — Dura Tech® mx

1 Batch Sensitivity : Finishes are batch sensitive (may have color variation) and

Cool Metallic Silver 1

65 50  ●  ●  ●

●	●  ●  ●  ●  ●

●  ●  ●

are directional in nature. Different batches

Cool ZACtique® II 1	39 22 ● ● ●	●	● ● ● ●	● ● Cool Metallic Champagne 1 54 33 ● ● ●	●	● ● ● ●	● ● Cool Metallic Copper 1	 53  29  ●  ●  ●	●	●  ●  ●  ●	 ●  ●
Premium Colors

Vintage® 1	22  20  ●  ●  ●	●	●  ●  ●  ●	●  ●
Carbon - Natural Matte®	NA  4  ●  ●  ●    ●    ●	●
Shale - Natural Matte®	41  23  ●  ●  ●    ●    ●	●
Unpainted Products

ZINCALUME® Plus 1	64  67  ●  ●  ●  ●  ●  ●  ●	●  ●	●
Pre-Primer	NA NA	●
REPRESENTATION OF COLORS MAY VARY DUE TO PRINTING LIMITATIONS
Request physical color chip samples at www.aepspan.com/sample-request
SPECIALTY PRINTS, ALUMINUM, CUSTOM COLORS, AND HEAVIER GAUGES AVAILABLE BY SPECIAL ORDER

DURA TECH®

Inquire with your sales representative for lead times and minimum order requirements.

are not to be mixed on projects. AEP Span recommends requesting a sample before ordering to ensure color accuracy. AEP Span is not responsible for color variations.
Oil Canning : All flat metal surfaces can display waviness commonly referred to as oil canning. Oil canning is an inherent characteristic of metal products, not a defect, and therefore is not a cause for panel rejection.

SRI values in accordance with ASTM E1980 and are based on independent testing. Cool Roof Rating Council (CRRC) performance values for CA Title 24 are based on color families and will differ from values in table.

DURA TECH®

Cool

Cool

FINISHES DEVELOPED BY

5000

mx

ZINCALUME® Plus

©2026 ASC Profiles, LLC. All rights reserved. ZINCALUME® is a registered trademark of BlueScope Steel Ltd. TruZinc®, Vintage®, & Natural Matte® are registered trademarks of Steelscape, LLC. All information stated in the color chart is correct at time of printing and subject to change without notice. Check website for the latest version. 0526 15k (CC046)

www.aepspan.com

800-733-4955

®

Dura Tech® coatings pair the proven corrosion resistance of a ZINCALUME® substrate with a PVDF resin (polyvinylidene fluoride) and cool pigment technology for lasting color retention and energy efficiency.

Dura Tech® 5000 and Dura Tech® mx	ASTM1	PERFORMANCE	
Standard Film Thickness	D5796	0.15 - 0.25 mil primer, 0.70 - 0.80 mil top coat
0.50 mil backer coat (Polyester system applied over a primer)	
Environment Film Thickness	D5796	Thick film primers, clear coats, or specialized pigmentation are available for unusual environmental conditions.	
Specular Gloss	D523	8-15% at 60o (Dura Tech® 5000) 15-30% at 60o (Dura Tech® mx)	
Pencil Hardness	D3363	F-2H	
Flexibility T-Bend	D4145	2T No loss of adhesion or evidence of cracking2	
Cross Hatch Adhesion	D3359	No adhesion loss	
Reverse Impact	D2794	No cracking or loss of adhesion	
Abrasion, Falling Sand	D968	65 liters minimum	
Flame Test	E84	Class A coating	
Acid Pollutants
20% Sulfuric Acid, 18hrs. 10% Muriatic Acid, 24hrs.	D1308	
No bleaching
No color change, no blistering	
Acid Rain Test	Kesternich	15 cycles minimum	
Alkali Resistance	Kesternich	No effect	
Salt Spray Resistance	B117	Passes 1,000 hours, coated steel2	
Cyclic Salt Fog	B5894	2,000 hours passes adhesion	
Humidity Resistance: 100% RH at 100o F	B2247	Passes 2,000 hours, coated steel2	
South Florida Exposure	D2244	<5 NBS units change	
UVB	D822	Passes 3,000 hours	
Chalk Resistance	D4214	Rating of 8 minimum	
ZINCALUME® substrate	A792	55% aluminum-zinc alloy coated steel
with a metallic coating weight of AZ50	SM	
FINISH WARRANTIES	
Limited warranties for chalk, fade, and film integrity are available in durations of up to 40-years for Dura Tech® 5000, Dura Tech® 5000P, and Dura Tech® mx. All AEP Span panels with a ZINCALUME® substrate is offered with a corrosion warranty.
Terms can be affected by factors such as environment and building use. The warranty for Vintage varies. Inquire for details.	
COMPOSITION & APPLICATION	
Dura Tech® coatings are factory-applied by oven-cured formulas processed by approved coil coaters. They utilize Kynar 500® or Hylar 5000® PVDF resins and inorganic, IR reflective pigments for superior long-term performance.	
PRETREATMENT	
All substrates are pretreated in accordance with paint manufacturer’s instructions. The pretreatment is to provide a suitable surface for application of the recommended primer.	
METALLIC COATINGS	
Minor differences in both color and appearance are normal and to be expected with metallic coatings. It is virtually impossible to match one batch to another. Due to the coil application process, striations and longitudinal patterning may also show on these products. To minimize the visual effects of the normal minor differences in paint and its application, an entire job should be painted at one time. Additionally, fabricated panels, flat sheets, and flashings should be orientated in the same direction for installation. AEP Span recommends requesting a sample before ordering to ensure color accuracy. AEP Span is not responsible for color variations.	
VINTAGE®: An innovative 24ga finish with a FEVE paint system on a TruZinc® G90 substrate with graffiti-resistant qualities.	
Vintage specifications and warranty vary from those stated above. Visit www.aepspan.com/warranties for details.	
1 All tests performed to latest ASTM revision. The test results set forth are representative of the results obtained by the paint manufacturer.

DU

2 Performances on HDG G90, ZINCALUME®, Galvalume®.

©2026 ASC Profiles, LLC. All rights reserved. ZINCALUME® is a registered trademark of BlueScope Steel Ltd. Galvalume® is a registered trademark of BIEC International, Inc. TruZinc®, Vintage®, & Natural Matte® are registered trademarks of Steelscape, LLC. Kynar 500® is a registered trademark of Arkema Inc. Hylar 5000® is a registered trademark of Solvay Specialty Polymers USA, LLC. All information stated in the color chart is correct at time of printing and subject to change without notice. Check website for the latest version. 0526 15k (CC046)

www.aepspan.com

800-733-4955

Premium Metal Roofing & Siding

Dura Tech® Coatings

®

DU

5000

mx

Cool

RA TECH®

Cool

RA TECH®

FINISHES DEVELOPED BY

®