DURA TECH™ 5000 - Premium 70% Fluoropolymer (PVDF) Coating

(Subject to upcharge)

 	 	 	

ZINCALUME® Plus*
SRI: 64 • LRV: 67 • GA: 24, 22, & 20

Cool REGAL WHITE
SRI: 88 • LRV: 75 • GA: 24 & 22

Cool PARCHMENT
SRI: 58 • LRV: 40 • GA: 24 & 22

VINTAGE®1
SRI: 22 • LRV: 20 • GA: 24
Vintage coated metal is an innovative coating process over a TruZinc® G90 metallic coated steel surface producing a beautiful, durable, aged-metallic finish.

Cool SIERRA TAN
SRI: 55 •  LRV: 34 •  GA: 24  &  22

Cool WEATHERED COPPER
SRI: 34 •  LRV: 11 •  GA: 24  &  22

Cool COLONIAL RED
SRI: 35 • LRV: 9 • GA: 24 & 22

Cool SLATE GRAY
SRI: 33 • LRV: 12 • GA: 24 & 22

Cool PEBBLE
SRI: 48 • LRV: 27 • GA: 24 & 22

Cool DARK BRONZE
SRI: 32 • LRV: 8 • GA: 24 & 22

Cool OLD TOWN GRAY
SRI: 43 •  LRV: 27 •  GA: 24  &  22

Cool MIDNIGHT BRONZE
SRI: 27 •  LRV: 7  •  GA: 24 &  22

Cool WALNUT
SRI: 38 • LRV: 18 • GA: 24 & 22

Cool TERRA-COTTA
SRI: 41 • LRV: 15 • GA: 24 & 22

Cool ZINC GRAY
SRI: 39 • LRV: 20 • GA: 24 & 22

Cool MATTE BLACK
SRI: 29 • LRV: 5 • GA: 24 & 22

METALLIC COLORS1
DURA TECH™ mx - Premium Fluoropolymer (PVDF) Pearlescent Coating (Subject to upcharge)

Cool METALLIC SILVER1
SRI: 65 •  LRV: 50 •  GA: 24  &  22

Cool SILVERSMITH1
SRI: 58 • LRV: 54 • GA: 24 & 22

Cool ZACtique®  II1
SRI: 39 • LRV: 22 • GA: 24 & 22

 	 	 	

Cool TAHOE BLUE
SRI: 33 • LRV: 14 • GA: 24 & 22

Cool LEAF GREEN
SRI: 30 • LRV: 11 • GA: 24 & 22

Cool REGAL BLUE
SRI: 29 • LRV: 10 • GA: 24 & 22

Cool FOREST GREEN
SRI: 29 • LRV: 9 • GA: 24 & 22

Cool SAGE GREEN
SRI: 41 •  LRV: 21 •  GA: 24  &  22

1 Please note that these colors are batch sensitive (may have color variation) and are directional in nature. Different batches are not to be mixed on projects. We recommend that you request a sample of current stocked material to review actual color before ordering to ensure color accuracy. We are not responsible for color variations.
* Clear acrylic coated

Cool METALLIC CHAMPAGNE1
SRI: 54 •  LRV: 33 •  GA: 24  &  22

Cool METALLIC COPPER1
SRI: 53 •  LRV: 29 •  GA: 24  &  22

STANDARD COLORS

PREMIUM COLOR1

Architectural Metal Roofing and Siding
COLOR CHART

Sample color chips are available upon request. Consult your AEP Span representative for more information.

800-733-4955

Custom colors available by request

www.aepspan.com

REPRESENTATION OF COLORS MAY VARY DUE TO PRINTING LIMITATIONS.

5000
Dura Tech™  coatings combine the corrosion protection of a ZINCALUME®  substrate with a highly durable resin formulation and cool pigment technology to provide excellent color retention and reduces the demand for energy.

DURA TECH 5000 and DURA TECH	mx	ASTM2	PERFORMANCE	
Standard Film Thickness	D5796	0.15 - 0.25 mil primer, 0.70 - 0.80 mil top coat
0.50 mil backer coat (Polyester system applied over a primer)	

Specular Gloss	D523	8-15% at 60º (Dura Tech 5000)
15-25% at 60º (Dura Tech mx)	
Pencil Hardness	D3363	F-2H	
Flexibility T-Bend	D4145	2T No loss of adhesion or evidence of cracking3	
Cross Hatch Adhesion	D3359	No adhesion loss	
Reverse Impact	D2794	No cracking or loss of adhesion	
Abrasion, Falling Sand	D968	65 liters minimum	
Flame Test	E84	Class A coating	
Acid Pollutants
20% Sulfuric Acid, 18hrs. 10% Muriatic Acid, 24hrs.	D1308	
No bleaching
No color change, no blistering	
Acid Rain Test	Kesternich	15 cycles minimum	
Alkali Resistance	Kesternich	No effect	
Salt Spray Resistance	B117	Passes 1,000 hours, coated steel3	
Cyclic Salt Fog	B5894	2,000 hours passes adhesion	
Humidity Resistance @ 100o	B2247	Passes 2,000 hours, coated steel3	
South Florida Exposure	D2244	<5 NBS units change	
UVB	D822	Passes 3,000 hours	
Chalk Resistance	D4214	Rating of 8 minimum	
ZINCALUME®	A792	55% aluminum-zinc alloy coated steel
and Galvalume® substrate	with a metallic coating weight of AZ50	SM
FINISH WARRANTIES
Limited warranties for chalk, fade and film integrity are available in durations of up to 40 years for both Dura Tech™ 5000 and Dura Tech™ mx. All AEP Span panels are offered with a corrosion warranty on Galvalume® or ZINCALUME® substrate. Terms can be affected by factors such as environment and building use. Vintage warranty varies.  Inquire  for details.
COMPOSITION & APPLICATION:
Dura Tech™ 5000/mx coatings are factory applied, oven cured formulas applied by approved coil coaters. They utilize Kynar 500® or Hylar 5000® PVDF resins and inorganic, IR reflective pigments for superior long-term performance.
PRETREATMENT
All substrates are pre-treated in accordance with paint manufacturer’s instructions. The pretreatment is to provide a suitable surface for application of the recommended primer.
METALLIC COATINGS
With metallic coatings, minor differences in both color and appearance are normal and to be expected. It is virtually impossible to match one metallic coating to another. Due   to the coil application process, striations and longitudinal patterning may also show on these products. To minimize the possible visual effects of the normal minor differences   in paint and its application, an entire job should be painted at one time. Additionally, fabricated panels, flat sheets, and flashings should be orientated in the same direction for installation. Contact AEP Span representative for actual color samples prior to purchase.
VINTAGE - Vintage coated metal is an innovative coating process over a TruZinc® G90 metallic coated steel surface producing a beautiful, durable, aged-metallic finish. Vintage specifications and warranty vary slightly from those stated above. Please visit www.aepspan.com/resource-center/warranties for details or contact an
AEP Span representative for details.	

Marine Environment Film Thickness	D5796	0.70 - 0.80 mil primer, 0.70 - 0.80 mil topcoat, 0.40 - 0.50 mil clear coat Other unusual environmental conditions or specialized pigmentation may have different primer and clear coat requirements.

2 All tests performed to the latest ASTM revision. The test results set forth are representative of the results obtained by the paint manufacturer.
3 Performances on HDG G90, ZINCALUME®, Galvalume®.

SRI=Solar Reflective Index. LRV=Light Reflectance Value. GA= Gauge of Steel.
SRI values in accordance with ASTM E1980 and are based on independent testing. Cool Roof Rating Council (CRRC) performance values
(for CA Title 24, Energy Star) are based on color families and will differ from those listed above. Please visit www.aepspan.com for additional information.

DURA TECH™ Fluoropolymer Coatings

©2019 ASC Profiles LLC. All rights reserved. ZINCALUME® is a registered trademark of BlueScope Steel Ltd. Galvalume® is a registered trademark of BIEC International, Inc. TruZinc® is a registered trademark of Steelscape, LLC Kynar 500® is a registered trademark of Arkema Inc. Hylar 5000® is a registered trademark of Solvay Specialty Polymers USA, L.L.C.
All information stated in the color chart is correct at time of printing and subject to change without notice, check our website for the latest version. 0919 web (CC046)

800-733-4955
www.aepspan.com