STANDARD COLORS
DURA TECH™ 5000 - Premium 70% Fluoropolymer (PVDF) Paint system

PREMIUM COLOR1
(Subject to upcharge)

ZINCALUME® Plus*
SRI: 64 • LRV: 67

Cool REGAL WHITE
SRI: 88 • LRV: 75

Cool PARCHMENT
SRI: 58 • LRV: 40

VINTAGE®1
SRI: 22 • LRV: 20

Cool SIERRA TAN
SRI: 55 • LRV: 34

Cool WEATHERED COPPER
SRI: 34 • LRV: 11

Cool COLONIAL RED
SRI: 35 • LRV: 9

Cool SLATE GRAY
SRI: 33 • LRV: 12

Cool TAHOE BLUE
SRI: 33 • LRV: 14

Cool LEAF GREEN
SRI: 30 • LRV: 11

Cool PEBBLE
SRI: 48 • LRV: 27

Cool DARK BRONZE
SRI: 32 • LRV: 8

Cool OLD TOWN GRAY
SRI: 43 • LRV: 27

Cool MIDNIGHT BRONZE
SRI: 27 • LRV: 7

Cool REGAL BLUE
SRI: 29 • LRV: 10

Cool FOREST GREEN
SRI: 29 • LRV: 9

Cool WALNUT
SRI: 38 • LRV: 18

Cool TERRA-COTTA
SRI: 41 • LRV: 15

Cool ZINC GRAY
SRI: 39 • LRV: 20

Cool MATTE BLACK
SRI: 29 • LRV: 5

Cool SAGE GREEN
SRI: 41 • LRV: 21

PRE-PRIMER
(PRE-PRIMED 2 SIDES)

METALLIC COLORS1
DURA TECH™ mx
Premium Fluoropolymer (PVDF) Pearlescent Paint system (Subject to upcharge)

Cool METALLIC SILVER1
SRI: 65 • LRV: 50

Cool SILVERSMITH1
SRI: 58 • LRV: 54

Cool ZACtique® II1
SRI: 39 • LRV: 22

Cool METALLIC CHAMPAGNE1
SRI: 54 • LRV: 33

Cool METALLIC COPPER1
SRI: 53 • LRV: 29

COLOR CHART

Architectural Metal Roofing and Siding

®

REPRESENTATION OF COLORS MAY VARY DUE TO PRINTING LIMITATIONS.
Sample color chips are available upon request. Consult your AEP Span representative for more information.

800-733-4955	Custom colors available by request

www.aepspan.com

	
PAINT SYSTEM	SMP	PVDF	
OVERALL	Better	Best	
PRICE POINT	Moderate	Higher	
WARRANTY	Long	Longest	

DURABILITY	Improved Weatherability	Highest Weatherability	

APPLICATION	Residential & Commercial	High-end, Architectural/ Commercial	

OTHER ATTRIBUTES	Wide range of colors
& gloss options	Excellent chalk & fade resistance	

REPRESENTATION OF COLORS MAY VARY DUE TO PRINTING LIMITATIONS
Sample color chips are available upon request. Consult your AEP Span representative for more information.
SPECIALTY PRINTS, ALUMINUM, CUSTOM COLORS, AND OTHER GAUGES AVAILABLE AS SPECIAL ORDERS
Inquire with your outside sales representative about lead times and minimum order requirements.

DURA TECH™ 5000: A premium 70% Fluoropolymer (PVDF) paint system.

DURA TECH™ 5000 (PVDF)	SRI	LRV	Des	Span	Sel	Fle	Pres	Per	Flus	HR-	Box	Nu-W	PBR	U-P	Mini	Flat	Flat	
	Cool Regal White*	88	75	​	​	​		​		​	​	​	​	​	​	​	​	​	
	Cool Parchment	58	40	​	​	​		​		​	​	​	​				​	​	
	Cool Sierra Tan	55	34	​	​	​		​		​	​	​	​				​	​	
	Cool Pebble	48	27	​	​	​		​		​								​	
	Cool Walnut	38	18	​	​	​		​		​								​	
	Cool Weathered Copper	34	11	​	​	​		​		​	​	​	​				​	​	
	Cool Dark Bronze	32	8	​	​	​		​		​	​	​	​				​	​	
	Cool Terra-Cotta	41	15	​	​	​		​		​	​	​	​				​	​	
	Cool Colonial Red	35	9	​	​	​		​		​								​	
	Cool Old Town Gray	43	27	​	​	​		​		​	​	​	​				​	​	
	Cool Zinc Gray	39	20	​	​	​		​		​	​	​	​				​	​	
	Cool Slate Gray	33	12	​	​	​		​		​	​	​	​				​	​	
	Cool Midnight Bronze	27	7	​	​	​		​		​	​	​	​				​	​	
	Cool Matte Black*	29	5	​	​	​		​		​	​	​	​				​	​	
	Cool Tahoe Blue	33	14	​	​	​		​		​	​	​	​				​	​	
	Cool Regal Blue	29	10	​	​	​		​		​	​	​	​				​	​	
	Cool Sage Green	41	21	​	​	​		​		​	​	​	​				​	​	
	Cool Leaf Green	30	11	​	​	​		​		​	​	​	​				​	​	
	Cool Forest Green	29	9	​	​	​		​		​	​	​	​				​	​	
DURA TECH™ mx (PVDF)1		
	Cool Metallic Silver	65	50	​	​	​		​		​	​	​	​				​	​	
	Cool Silversmith	58	54	​	​	​		​		​								​	
	Cool ZACtique® II	39	22	​	​	​		​		​	​	​	​				​	​	
	Cool Metallic Champagne	54	33	​	​	​		​		​	​	​	​				​	​	
	Cool Metallic Copper	53	29	​	​	​		​		​								​	
PREMIUM COLOR 1		
	Vintage®	22	20																
BARE (Clear Acrylic Coated)		
	ZINCALUME® Plus	64	67	​	​	​	​	​	​	​	​	​	​	​	​	​	​	​	
PRE-PRIMER		
Pre-Primed Two Sides	N/A	N/A																

DURA TECH™ mx: A premium Fluoropolymer (PVDF) Pearlescent paint system.
VINTAGE® COATED METAL: TruZinc® G90
substrate with a FEVE paint system and graffiti-resistant qualities.
* AVAILABLE IN ALUMINUM .040” ONLY:
Stocked in Matte Black and Regal White, and is available in 48” x 10’ flat sheet.
Material is painted on both sides. One side is Matte Black and the other is Regal White.
1 BATCH SENSITIVITY: Prints and metallic paint systems are batch sensitive (may have color variation) and are directional in nature. Different batches are not to be mixed on projects. AEP Span recommends requesting a sample before ordering to ensure color accuracy. AEP Span is not responsible for color variations.
OIL CANNING: All flat metal surfaces can display waviness commonly referred to as “oil canning”. “Oil canning” is an inherent characteristic of steel products, not a defect, and therefore is not a cause for panel rejection.

SRI values in accordance with ASTM E1980 and are based on independent testing. Cool Roof Rating Council (CRRC) performance values for CA Title 24 are based on color families and will differ from those listed in table.

FINISHES DEVELOPED BY

DURA TECH™ Fluoropolymer Coatings

TABLE NOTES:
24 and 22 GA
24 GA only 22 GA only
SRI: Solar Reflective Index.
LRV: Light Reflectance Value.

®

®

ign Span®
-Lok™ hp ect Seam® x Series
tige Series® ception Collection® h Panel
36® Rib™
ave® Corrugated Panel
anel
-V-Beam™ Sheet 46"
Sheet 48 3⁄8"

5000

©2024 ASC Profiles LLC. All rights reserved. ZINCALUME® is a registered trademark of BlueScope Steel Ltd. Galvalume® is a registered trademark of BIEC International, Inc. TruZinc® is a registered trademark of Steelscape, LLC Kynar 500® is a registered trademark of Arkema Inc. Hylar 5000® is a registered trademark of Solvay Specialty Polymers USA, L.L.C.
All information stated in the color chart is correct at time of printing and subject to change without notice, check our website for the latest version. 0224 web (CC046)

ZINCALUME® Plus
800-733-4955
www.aepspan.com

Dura Tech™ coatings combine the corrosion protection of a ZINCALUME® substrate with a highly durable resin formulation and cool pigment technology to provide excellent color retention and reduces the demand for energy.

DURA TECH 5000 and DURA TECH mx	ASTM2	PERFORMANCE	
Standard Film Thickness	D5796	0.15 - 0.25 mil primer, 0.70 - 0.80 mil top coat
0.50 mil backer coat (Polyester system applied over a primer)	

coat

Specular Gloss	D523	8-15% at 60º (Dura Tech 5000) 15-25% at 60º (Dura Tech mx)	

Pencil Hardness	D3363	F-2H		
Flexibility T-Bend	D4145	2T No loss of adhesion or evidence of cracking	3	
Cross Hatch Adhesion	D3359	No adhesion loss		
Reverse Impact	D2794	No cracking or loss of adhesion		
Abrasion, Falling Sand	D968	65 liters minimum		
Flame Test	E84	Class A coating		
Acid Pollutants
20% Sulfuric Acid, 18hrs. 10% Muriatic Acid, 24hrs.	D1308	
No bleaching		
Acid Rain Test	Kesternich	15 cycles minimum		
Alkali Resistance	Kesternich	No effect		
Salt Spray Resistance	B117	Passes 1,000 hours, coated steel3		
Cyclic Salt Fog	B5894	2,000 hours passes adhesion		
Humidity Resistance @ 100o	B2247	Passes 2,000 hours, coated steel3		
South Florida Exposure	D2244	<5 NBS units change		
UVB	D822	Passes 3,000 hours	

SM	
Chalk Resistance	D4214	Rating of 8 minimum		

Marine Environment Film Thickness	D5796	0.70 - 0.80 mil primer, 0.70 - 0.80 mil topcoat, 0.40 - 0.50 mil clear Other unusual environmental conditions or specialized pigmentation may have different primer and clear coat requirements.

No color change, no blistering

ZINCALUME®
and Galvalume® substrate	A792	55% aluminum-zinc alloy coated steel with a metallic coating weight of AZ50	
FINISH WARRANTIES	
Limited warranties for chalk, fade and film integrity are available in durations of up to 40 years for both Dura Tech™ 5000 and Dura Tech™ mx. All AEP Span panels are offered with a corrosion warranty on Galvalume® or ZINCALUME® substrate. Terms can be affected by factors such as environment and building use. Vintage warranty varies. Inquire for details.	
COMPOSITION & APPLICATION:	
Dura Tech™ 5000/mx coatings are factory applied, oven cured formulas applied by approved coil coaters. They utilize Kynar 500® or Hylar 5000® PVDF resins and inorganic, IR reflective pigments for superior long-term performance.	
PRETREATMENT	
All substrates are pre-treated in accordance with paint manufacturer’s instructions. The pretreatment is to provide a suitable surface for application of the recommended primer.	
METALLIC COATINGS	
With metallic coatings, minor differences in both color and appearance are normal and to be expected. It is virtually impossible to match one metallic coating to another. Due to the coil application process, striations and longitudinal patterning may also show on these products. To minimize the possible visual effects of the normal minor differences in paint and its application, an entire job should be painted at one time. Additionally, fabricated panels, flat sheets, and flashings should be orientated in the same direction for installation. Contact AEP Span representative for actual color samples prior to pur- chase.	
VINTAGE - Vintage coated metal is an innovative coating process over a TruZinc® G90 metallic coated steel surface producing a beautiful, durable, aged-metallic finish.	
Vintage specifications and warranty vary slightly from those stated above. Please visit www.aepspan.com/resource-center/warranties for details or contact an AEP Span representative for details.	
2 All tests performed to the latest ASTM revision. The test results set forth are representative of the results obtained by the paint manufacturer.
3 Performances on HDG G90, ZINCALUME®, Galvalume®.
SRI=Solar Reflective Index.  LRV=Light Reflectance Value.  GA= Gauge of Steel.
SRI values in accordance with ASTM E1980 and are based on independent testing. Cool Roof Rating Council (CRRC) performance values
(for CA Title 24, Energy Star) are based on color families and will differ from those listed above. Please visit www.aepspan.com for additional information.
FINISHES DEVELOPED BY

®.

®	®

www.aepspan.com

5000

DURA TECH™5000/mx (PVDF) Fluoropolymer Coatings Technical Data

®

All information stated in the color chart is correct at time of printing and subject to change without notice, check our website for the latest version. 0224 web (CC046)

©2024 ASC Profiles LLC. All rights reserved. ZINCALUME® is a registered trademark of BlueScope Steel Ltd. Galvalume® is a registered trademark of BIEC International, Inc. TruZinc® is a registered trademark of Steelscape, LLC Kynar 500® is a registered trademark of Arkema Inc. Hylar 5000® is a registered trademark of Solvay Specialty Polymers USA, L.L.C.

800-733-4955