Not all colors and profiles are available at all locations. Please see back of color chart for details.
We recommend requesting a physical sample to review color before ordering. We are not responsible for color variations.

ZINCALUME® Plus 1 3
SRI: 64 • LRV: 67

Cascade Gray
SRI: 58 • LRV: 41

Matte Black 2
SRI: NA • LRV: 5

Weathered Copper
SRI: 32 • LRV: 11

Winter White
SRI: 88 • LRV: 74

Taupe
SRI: 53 • LRV: 28

Canyon Red
SRI: 45 • LRV: 16

Slate Gray
SRI: 32 • LRV: 13

Surf White
SRI: 74 • LRV: 59

Patina Steel
SRI: 38 • LRV: 17

Rustic Red
SRI: 43 • LRV: 13

Tahoe Blue
SRI: 33 • LRV: 14

Light Stone
SRI: 70 • LRV: 53

Chestnut Brown
SRI: 36 • LRV: 12

Old Town Gray
SRI: 43 • LRV: 27

Everglade
SRI: 35 • LRV: 19

Desert Beige
SRI: 58 • LRV: 39

Classic Brown
SRI: 29 • LRV: 7

Old Zinc Gray
SRI: 43 • LRV: 22

Denali Green
SRI: 29 • LRV: 11

	

Forest Green
SRI: 36 • LRV: 8

PREMIUM COLOR

Copper Penny 3

MEASURED ON A SCALE OF 0 - 100
Light Reflective Value (LRV)
Measures the percentage of visible light reflected from a surface (0-100). Higher values indicate lighter colors.
Solar Reflective Index (SRI)
Indicates how well a surface reflects and releases solar heat. Higher values result in better thermal performance and cooler surface temperatures, helping cut down on energy cooling costs.

SRI: 53 • LRV: 28

UNPAINTED & UNCOATED

Natural Rust 3
SRI: 30 • LRV: 12
(Subject to upcharge)

IronOx 4
SRI: NA • LRV: NA

SRI values in accordance with ASTM E1980 and are based on independent testing. Cool Roof Rating Council performance values (for CA Title 24) are based on color families and can differ from above.

FINISHES DEVELOPED BY

Metal Roofing and Siding Solutions

®

STANDARD COLOR CHART

Customer Service Centers
Salem, OR: 800-272-7023 I Spokane, WA: 800-776-8771

www.ascbp.com

1 Unpainted with a clear acrylic coating.	®
2 Matte Black is not a rated product by the Cool Roof Rating Council (CRRC).
3 Color is batch sensitive (may have color variation) and is directional in nature. Different batches are not to be mixed on projects.
4 IronOx is black steel (uncoated and unpainted), that rusts naturally. No warranty. Only available in 22 gauge Nu-Wave® Corrugated.
REPRESENTATION OF COLORS MAY VARY DUE TO PRINTING LIMITATIONS.
Sample color chips are available upon request. Contact a ASC Building Products representative for more information.

Metal Roofing and Siding Solutions	®
STANDARD COLOR CHART

36" - PBR Panel
36" - Nu-Wave® Corrugated

Paint System Color Key

12" - Skyline Roofing®
16" - Skyline Roofing®

24" - 21/2" Corrugated

Dura Tech® xl

36" - Delta Rib™ III

(SMP)

24" - Delta Rib™

36" - Nor-Clad®

36" - Strata Rib®

ColorGuard 25 with Spectrascape®
(Polyester)
Dura Tech® nt
(SMP)
ZINCALUME® Plus
(Unpainted with a clear acrylic coating)
Premium Color
(Subject to upcharge)

Colors & Gauges

ZINCALUME® Plus 3
Winter White

Light Stone Desert Beige Cascade Gray
Taupe Patina Steel Chestnut Brown Classic Brown Matte Black 2 Canyon Red Rustic Red
Old Town Gray Old Zinc Gray Weathered Copper

Slate Gray Tahoe Blue Everglade Denali Green Forest Green

Natural Rust 3
IronOx 4
Production Location Key
CA - West Sacramento, California OR - Salem, Oregon
WA - Spokane, Washington

26	26

29	26	29

1	WA

WA

1

26	29	26

OR WA

WA

OR WA
OR

OR WA

OR WA
OR WA

OR

OR WA
OR WA

WA
WA

29	26	29

WA
OR

WA

OR

WA

WA WA

OR

WA WA
OR

WA

26	26	26

4

Salem
West Sacramento, Salem, Spokane

West Sacramento

West Sacramento, Spokane
West Sacramento

West Sacramento, Salem, Spokane

West Sacramento, Salem

West Sacramento, Salem, Spokane

West Sacramento, Salem

Salem

West Sacramento

West Sacramento

1 Available in 32" net coverage only.
2 Matte Black is not a rated product by the Cool Roof Rating Council (CRRC).
3 Color is batch sensitive (may have color variation) and is directional in nature. Different batches are not to be mixed on projects.
4 IronOx is black steel (uncoated and unpainted), that rusts naturally. No warranty. Only available in 22 gauge Nu-Wave® Corrugated. We recommend requesting a physical sample to review color before ordering. We are not responsible for color variations.

All information stated in the color card is correct at time of printing and subject to change without notice.
Spectrascape® is a registered trademark of Steelscape, LLC. ZINCALUME® is a registered trademark of BlueScope Steel Ltd.
©2026 ASC Profiles, LLC All rights reserved. 0726  web (CC150)

www.ascbp.com