®

NOR-CLAD®

Customer Service Centers
Salem, OR: 503-390-7174 or 800-272-7023 I Spokane, WA: 509-536-4097 or 800-776-8771

www.ascbp.com

Nor-Clad
Nor-Clad is a light gauge, exposed fastened 36" wide panel used for roof or wall applications in residential, light-commercial and agricultural projects.
FEATURES AND BENEFITS
36" coverage roof and wall panel.
Roof Installation: Minimum 3:12 recommended. Wall Installation: Horizontal or Vertical.
26 and 29ga in Dura Tech™ xl, ColorGuard 25 and in ZINCALUME® Plus.
Limited Lifetime Warranty for residential applications.
Custom manufactured panel lengths: 4'-6" to 45'-0".
Matching polycarbonate panels available.
Roof assemblies Class A Fire Rated when installed on non-combustible deck or framing per IBC or IRC or when installed in accordance to UL listings (UL790). Wall assemblies rated for fire resistance (UL263) when installed in accordance with UL listings.
Class 4 Impact (Hail) Resistance rated per UL 2218.
Panel evaluated by accredited third party. All structural performance data is contained within Building Code Approval Report: IAPMO-UES #ER-0550.

STANDING BY OUR PRODUCTS AND WARRANTIES FOR 50 YEARS

5⁄8"	9"

 36" Net Coverage 

ZINCALUME® Plus
Winter White Surf White Light Stone Desert Beige Cascade Gray
Taupe Patina Steel Chestnut Brown Classic Brown Matte Black Canyon Red Rustic Red
Old Town Gray
Old Zinc Gray Weathered
Copper
Slate Gray Tahoe Blue Everglade Denali Green Forest Green
Copper Penny*
Premium Color –
Natural Rust*
(subject to upcharge)

Gauge	
Span	
Cond.	Positive (Inward) Uniform Load Capacity (lbs/ft2) / Span (ft.-in.)	
			16"	2'-0"	2′-6"	3'-0"	3'-6"	4'-0"	4'-6"	5'-0"	6'-0"	

29	Single Span	ASD, W/Ω	199	88	56	39	29	22	17	14	10	
		L/180	-	87	45	26	16	11	8	6	3	
	Double Span	ASD, W/Ω	196	88	57	39	28	22	17	13	9	
		L/180	-	-	-	-	-	-	-	-	8	
	Triple Span	ASD, W/Ω	243	110	70	49	36	27	21	18	12	
		L/180	-	-	-	49	31	21	14	11	6	

26	Single Span	ASD, W/Ω	264	117	75	52	38	29	23	19	13	
		L/180	-	109	56	32	20	14	10	7	4	
	Double Span	ASD, W/Ω	248	111	71	50	36	28	22	17	12	
		L/180	-	-	-	-	-	-	-	17	10	
	Triple Span	ASD, W/Ω	307	138	89	61	45	34	27	22	15	
		L/180	-	-	-	61	38	26	18	13	8	

LOAD TABLE

SMP COLORS

Dura Tech™ xl	ColorGuard 25	

	AK, CA, OR, WA	CA, OR	AK, CA, OR, WA	
	AK, CA, OR, WA	CA, OR	OR, WA	
	OR, WA	—	—	
	AK	—	CA, OR, WA	
	AK, CA, OR, WA	—	OR, WA	
	OR	—	—	
	CA, OR, WA	—	—	
	CA, OR, WA	—	—	
	AK, CA, OR, WA	—	OR, WA	
	AK, CA, OR, WA	—	—	
	AK, CA, OR, WA	—	—	
	AK, CA, OR, WA	—	—	
	AK, CA, OR, WA	—	OR, WA	
	AK, CA, OR, WA	—	OR, WA	
	AK, CA, OR, WA	—	—	
	AK, CA, OR, WA	CA, OR	—	
	AK, CA, OR, WA	—	—	
	AK, CA, OR, WA	OR	—	
	AK, CA, OR, WA	—	—	
	AK, CA, OR, WA	CA, OR	OR, WA	
	AK, CA, OR, WA	—	OR, WA	
	AK, CA, OR, WA	—	—	
	AK, WA	—	AK, WA	

29 Gauge	26 Gauge	29 Gauge

Keeps the heat out and the color brilliant.

Superior color retention Chalk and fade resistant Energy saving colors.

COLORGUARD 25

®

Spweithctrascape
A robust and economical paint system.
Chalk and fade resistant
Resist peeling or cracking for 25 years.

REPRESENTATION OF COLORS MAY VARY DUE TO PRINTING LIMITATIONS.
Sample color chips are available upon request. Consult your ASC Building Products representative for more information.
* Please note these colors are batch sensitive (may have color variation) and are directional in nature. Different batches are not to be mixed on projects. We recommend that you request a sample of current stocked material to review actual color before ordering to ensure color accuracy. We are not responsible for color variations.
Manufacturing Locations:
AK - Anchorage, Alaska
CA - Sacramento, California OR - Salem, Oregon
WA - Spokane, Washington

Properties	
Gauge	Base Steel Thickness (in)	Yield (ksi)	Tensile (ksi)	Wt. (lbs/ft2)	I+
(in4/ft)	S+
(in3/ft)	I-
(in4/ft)	S-
(in3/ft)	
29	0.0139	80	82	0.65	0.0080	0.0147	0.0064	0.0149	
26	0.0173	80	82	0.81	0.0100	0.0195	0.0098	0.0188	

NOTES:
Top values based on allowable stress (ASD). Bottom values based on a deflection limit of L/180. “-” denotes that the allowable load is limited by the panel stress vs. deflection limit.
Steel conforms to ASTM A653 (Galvanized) or ASTM A792 (ZINCALUME) structural steel. Tabulated values are for positive (inward) uniform loading only.
Values are based on the American Iron and Steel Institute “Cold Formed Steel Design Manual” (AISI S100-16). Refer to ascbp.com for more complete Nor-Clad performance data.

NOTES: The moments of inertia, I+ and I-, presented for determining deflection are: (2IEffective + IGross)/3

Inward Loads	
Single Span	w, distributed load

L, span	
	
Double Span	w

L	L	
	
Triple Span	w

L	L	L	

All information stated in the product sheet is correct at time of printing and subject to change without notice, check our website for the latest version.

NOR-CLAD®

®

©2018-2024

ASC Profiles LLC. All rights reserved. ZINCALUME® is a registered trademark of BlueScope Spectrascape® is a registered trademark of Steelscape, LLC. 0224 web (PS220)

Steel Ltd.

www.ascbp.com