Features and Benefits
Material thickness*: 1", 1-1/2", 2"
Polyethylene foam for exceptional strength and compressibility
Interlocking dovetail connections available on many profiles
Resists damaging ultra violet rays and ozone deterioration
One person installation
Color: Charcoal
Available with adhesive applied to assure positive positioning during installation
Hundreds of profile configurations available
* Not all closure profiles available in all material thicknesses

Application
Designed to close gaps in roof and sidewall applications

Product Selection
Many profiles available to match most OEM panel profiles. Popular items listed.
Material No.	
Profile Description	Pieces / Carton	
Inner
with Adhesive	Inner
No Adhesive	Outer
with Adhesive	Outer
No Adhesive			
799586	799582	799598	799589	3/4" HiRib	100	
799448	799444	799457	799450	R panel	100	
799403	799399	799403	799399	2.67"x1/2" corrugated	100	
799434	799433	799434	799433	7.2 pitch	100	
799607	799605	799612	799609	M/U panel	100	
799570	799569	799577	799573	Pro Panel II	100	
799754	799752	799758	799755	5V Crimp	100	

Sold in full carton quantity only.

US
T 800 234 4533
us.sfs.com

Canada
T 866 847 5400
ca.sfs.com

Metric values are approximate conversions.

© SFS, 07/2021, US, V1.01

All information is non-binding and without guarantee. Before using the products, all specifications and calculations must be checked by a suitably qualified person and local regulations must be observed. This document is subject to revision. We reserve the right to make technical changes. (07/2021, V1.01)

Product Specifications	
Test	Test Method	Units	Values 1"	Values
1-1/2" & 2"	
Density	BS ISO 7214 1998	lb/ft³	1.5	1.8	
Working Temperature Range	Internal	°F	212 max	212 max	
			-94 min	-94 min	
Compression Deflection	25%	BS ISO 7214 1998	psi	7.7	9.3	
	50%			17.1	19.0	
Compression Set	25% - 1/2 hr	BS ISO 7214 1998	% set	13.0	10.5	
	25% - 24 hr			5	3	
Tear Strength	BS EN ISO 8067 1995	lb/in	2.8	4.2	
Tensile Strength	ISO 7214 1998	psi	46.4	54.4	
Elongation	%	130	140	
Flammability	FMVSS302	4"/min	Pass	Pass	
Shore Hardness	ISO 868 1985	OO	50	53	

Maximum service temperature is 212° F. Applications where service temperature exceeds 212° F should be avoided, as the material can experience thermal degradation.

Installation and Application Considerations
VistaFoam closure is not recommended for installation or placement beneath translucent or clear materials where it may be exposed to direct sunlight. The potential intensification of the sun's rays may result in increased temperatures which could effect the condition of the material.

Typical Inside Closure Application

Typical Outside Closure Application

 		

© SFS, 07/2021, US, V1.01

Step 1: Ensure the self-adhesive closure configuration fits the roof panel used.

Step 2: The inside closure fits the under- side of the panel. Position the honeycomb texture side outward for optimal UV protection.

Step 3: Place the roof panel over pre- cut closure configuration for a snug fit. Attach panel over closure with the proper fasteners.

US
T 800 234 4533
us.sfs.com

Canada
T 866 847 5400
ca.sfs.com

Metric values are approximate conversions.
All information is non-binding and without guarantee. Before using the products, all specifications and calculations must be checked by a suitably qualified person and local regulations must be observed. This document is subject to revision. We reserve the right to make technical changes. (07/2021, V1.01)